|  | APPROVED BY: SIGNATURE: DATE: |
| --- | --- |
| STANDARD OPERATING PROCEDURE | REVIEWED BY: DATE: |
| Capacity Test of Li-Ion Polymer Pouch Cell (Melasta SLPB9675175, 3.7 V 14 Ah, 20 C) using B&K Precision 8542B DC Electronic Load | AUTHOR: |
|  | ISSUE DATE: |
| This Standard Operating Procedure is to be reviewed every 2 years or whenever changes are required to the materials, equipment or procedure – whichever comes sooner. However, if a safety incident occurs while this SOP is being followed, this must be reviewed immediately. |  |

# PURPOSE

This SOP describes the safe procedure for performing capacity testing of Li-Ion polymer cells at 0.5 C discharge (≈7 A) to a 3.0 V cutoff using the Model 8542B (8500B Series) DC Electronic Load and proprietary battery test software.

# SCOPE

Applies to all laboratory personnel conducting capacity verification of Li-Ion pouch cells in the battery testing facility.

# REFERENCES

# Manufacturer datasheet: Melasta SLPB9675175 (14 Ah, 3.7 V, 20 C).

# Equipment manual: B&K Precision 8542B Electronic Load.

# University laboratory safety manual.

# DEFINITIONS

- C-rate: Charge/discharge current relative to nominal capacity (0.5 C ≈ 7 A for 14 Ah cell).

- Cutoff voltage: Minimum allowable discharge voltage (3.0 V).

- OCV: Open Circuit Voltage.

# Health and safety REQUIREMENTS

- Mandatory PPE: Safety glasses, cotton lab coat, insulated gloves, enclosed shoes.

- Additional PPE: Face shield during first cycles; respirator available for vent events.

- Induction: Staff must complete lithium-ion battery hazard training and lab induction.

Mandatory PPE comprising:

Safety glasses, heat-resistant gloves, enclosed shoes.

Additional PPE

# OPERATING PROCEDURE

## Pre-operation

## Inspect pouch cell for swelling, damage, or leaks. Do not use damaged cells.

## Place cell in fire-resistant, ventilated chamber.

## Connect cell tabs to insulated copper clamp fixture with Kelvin sense leads.

## Attach thermocouple to cell surface.

## Test setup
5. Program software:

## Discharge mode: CC 0.5 C (7 A).

## Voltage cutoff: 3.0 V.

## Data log: Voltage, current, capacity, temperature.

## Confirm cutoffs (upper 4.20 V, lower 3.0 V) and safety limits.

## Operation

## Start discharge sequence.

## Monitor voltage, current, and temperature during test.

## Stop test immediately if temperature >45 °C, voltage <3.0 V, or abnormal behavior observed.

## Shut Down

# After discharge completes, disconnect DC load.

# Allow cell to cool to ambient.

# Record final capacity (mAh, Wh) in test log.

# emergency Situations

- Thermal runaway / venting: Stop test, evacuate area, close hood, call UON Security (15888). Use Class D extinguisher if fire develops.

- Electrical fault: Hit emergency stop on DC load, disconnect mains.

- Exposure to smoke: Evacuate, call emergency services (000).

# Upset conditions

- Power failure: Ensure load input is off; do not reconnect until test plan is re-verified.

- Software crash: Abort test, safely disconnect cell, restart procedure.

# emergency CONTACTS

| Emergency Contacts | Name | Contact Number |
| --- | --- | --- |
| Emergency Call Services | Police Ambulance Fire Brigade | 0 000 ( mobile phone: 000 or 112) |
| UON Security Services | Emergency line CALLAGHAN | 4921 5888 / internal line 15888 |
| Contact (Supervisor) |  |  |
| First Aid Officers |  |  |
| Building Wardens |  |  |

| I have read and understood this Standard Operating Procedure and agree to follow the above-mentioned methodology and associated control measures. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Name: |  | Signature: |  | Date: |  |
| Name: |  | Signature: |  | Date: |  |
| Name: |  | Signature: |  | Date: |  |